## Slide 1: Core Thermal Design
Mohsin Mohd Sies
Muhammad Syahir Sarkawi
Universiti Teknologi Malaysia
mohsin@utm.my
http://www.mohsin-sies.com

## Slide 2: Motivation
Thermal (not nuclear) considerations limit the amount of reactor power generation
Temperatures anywhere in the core must not exceed material property limitations (fuel, cladding)
Otherwise fuel element damage might result in release of large quantities of radioactive material into coolant, or in-core fuel meltdown.

## Slide 5
Introduction

## Slide 6
Introduction
Reactors must be designed in such a way that the fission products always remain confined within the fuel; throughout
  the operational lifetime of the core,
  during shutdown,
  under accident conditions,
  when the fuel may be denied normal cooling
The reactor power generation is limited by thermal rather than nuclear

## Slide 7
Introduction
The accepted design criterion
  the integrity of the cladding must be maintained through all operations,
  the expansion of the fuel on melting cannot rupture the cladding,
  the fuel must not melt
The melting point of which depends on burnup; that is on the fraction of the fissile atoms that have undergone fission
  generally, between 5,000 - 5,100 (2,760 - 2,815 )
  maximum fuel temperature below 4,500 (2,480 )

## Slide 8
Introduction
In the HTGR, where the fuel consists of small particles of uranium and thorium dicarbide in a carbonaceous binder, the maximum fuel temperature is about 6,500 (3,600 )
Natural or enriched uranium metal melts at 2,070 (1,132 ), but it also undergoes two changes in solid phase (alteration in crystalline structure); at 1,234 (668 ) and at 1,425 (774 )
  However, above about 750 (400 ), the strength of the metal decreases rapidly
  This permits fission product gases to gather and diffuse into pockets in the fuel, which in turn leads to the expansion of the fuel and to cladding failure.

## Slide 9
Introduction
  Therefore, it is usual practice to design uranium metal-fueled reactors with maximum fuel temperatures below 750 (400 C)
  This low temperature is not a serious drawback in transferring heat to coolant
  The thermal conductivity of uranium metal is much higher than
  at 600 , for example, is 6.5 times higher for uranium metal than for

## Slide 10
General Considerations

## Slide 11
The rate at which heat is removed in a heterogeneous reactor core
First factor, , is governed (1) by the heat transfer by conduction through the fuel elements, cladding and other structures, if any separating these elements from the coolant and (2) the heat transfer be convection to the coolant
General Considerations
(1)
: Heat removal rate,
: Overall heat transfer coefficient=,
: Area across which heat is transferred,
: Mean temperature between heat generator and coolant,

## Slide 12
General Considerations
Coolant
Fuel pellet
Cladding
Small gap
Figure 1: Cross-sections of a conventional fuel pellet

## Slide 13
General Considerations
Fuel cladding should have high thermal conductivity
Other considerations should be taken into considerations such as low neutron absorption cross section, workability, withstand high temperatures and withstand corrosive action by coolant fluid.
Typical cladding materials, stainless steel, aluminum, zirconium and magnesium.
The resistance to heat conduction in the cladding is then reduced by holding the cladding thickness to a minimum.
The heat transfer by convection to the coolant is dependent on the coolant’s physical characteristics and on operating conditions, such as the coolant velocity
The second factor, , is the heat-transfer surface. The circumferential area of all the fuel elements, that must be designed within the reactor core
The third factor, , is the mean difference between the temperatures of the coolant and fuel.

## Slide 14
Core Thermal Design Considerations

## Slide 15: Core Thermal Design
Core thermal design is an art of compromise
An iterative process (interdependence of heat flux and water density)
Overall plant characteristics is influenced by thermal hydraulic considerations

## Slide 16: Core Thermal Design
Once core basic lattice has been determined from nuclear, hydraulic, and heat transfer, the overall size of core becomes a sole function of thermal considerations
Parameters
  Fuel temperature distribution (most important)
  Specific power
  Power density
  Heat flux

## Slide 17: Core Design Objectives
Maximize core power density
Maximize attainable fuel burnup
Minimize cost of electricity
High outlet temperature for higher thermal efficiency
But temperatures of fuel and cladding anywhere in core must not exceed safe limits (material limitation)

## Slide 18: Design Constraints

## Slide 19: Design Constraints

## Slide 20: Thermal Reactor Design
3 aspects of design considerations
  Nuclear Design
  Thermal-hydraulics Design
  Mechanical/Material Design

## Slide 21: Nuclear Design

## Slide 22: Thermal-hydraulics Design

## Slide 23: Mechanical/Materials Design

## Slide 24: Impact on various design areas

## Slide 25: Impact on various design areas

## Slide 26
Limits and
Safety Aspects

## Slide 27: Thermal Design Safety Aspects
DNB Ratio
Hot channel, hot spot factors
Thermal limits
  Fuel centerline temperature
  Cladding inner surface temperature
Values change with fuel burnup!

## Slide 28: Thermal Design Nomenclature (Nominal, Average, Peak, Maximum)

## Slide 29: Thermal Design Margin

## Slide 30: Thermal Design Limits

## Slide 31: Thermal Design Limits

## Slide 32
DNB Ratio

## Slide 33
Boiling Crisis for LWR

## Slide 34
Evaluation by Local Heat Flux (PWR)

## Slide 42: Thermal Crisis Summary
MDNBR > 1.17 (Japan)

## Slide 43
Hot Channel & Hot Spot Factor
Hot spot factor (hot-channel factor) is safety factor or margin multiplied to the calculated nominal fluxes.
In any reactor, the extent to which exceeds the average heat flux in the core is given by the hot channel factor, also called the hot spot factor, F.
(4)
: is the average heat flux in the core

## Slide 44: Hot-spot Factors
Deviation from nominal values are contributed by
  Nuclear hot-spot factors
  Engineering hot-spot factors

## Slide 45: Nuclear Hot-spot Factors
Deviations due to
  Partially inserted control rods
  Nonhomogeneities
    Moderator (boiling)
    Fuel
    Structural and other materials

## Slide 46: Engineering Hot-spot Factors
Deviations due to
  Mechanical subfactors
    Manufacturing tolerances (clad thickness)
    Warping of fuel elements
  Flow distribution subfactors
    Maldistribution of coolant flow
    Heat transfer coefficient, h
    Fuel element dimensions

## Slide 47
Manufacturing tolerances in the fuel assemblies ,may result in slight bowing of the fuel rods, leading to reduced coolant flow and excessive heating of a portion of the fuel.
Hot Channel & Hot Spot Factor
(Engineering Hot Spot Factor)

## Slide 48
Fluctuations in the thickness of the cladding may give rise to hot spots where the cladding is thinnest. (thin cladding leads to a larger gap, hence a larger between fuel pellet and cladding)
Also, certain aspects of the coolant flow are inherently statistical in character and tend to give fluctuations in the heat flux.
These various mechanisms by which differ from its computed value, describe by the engineering hot channel factor
Hot Channel & Hot Spot Factor
(Engineering Hot Spot Factor)

## Slide 49: Hot-spot Factors (classified by effects)
By effects on temperature or enthalpy of fuel and coolant
  Factor for temp. rise of coolant from core inlet conditions,
  Factor for temp. rise across coolant boundary layer,
  Factor for temp. rise across fuel element,

## Slide 51: Overall Hot-spot Factor
Combining hot-spot subfactors, f, to get overall hot-spot factor, F.
Methods;
  Multiplicative
    All deviation factors are assumed to take place simultaneously at the same point.
    Overly conservative result
  Statistical
    Many deviation factors are independent of each other
    Small probability of occurring at the same point
    More realistic result

## Slide 52
Hot Channel & Hot Spot Factor
(Overall Hot Spot Factor)
The overall hot channel is then
Each of the individual mechanisms is described, in turn, by an engineering hot channel factor,
The engineering subfactors are obtained from data on fabricated reactor components or from tests.
For instance, the amount of fissile material per unit length of the fuel rods. For a given thermal flux, is very nearly proportional to . When measurements of are carried out on manufactured rods, it is found that the actual values form a normal distribution about some mean or average value shown in Figure 3
(6)

## Slide 53
All values of are presumably possible. However, specific values of become less and less likely with increasing deviation from the mean.
Figure 3: Normal distribution of measured values of

## Slide 54
Hot Channel & Hot Spot Factor
It shown that probability that exceeds by more than , where is standard deviation pf the distribution (1.35 per 1,000 an unlikely occurrence)
In those situations like the one just described, in which is proportional to a normally distributed engineering variable , the engineering subfactor is defined as
(7)
: is the value of
: is the standard deviation

## Slide 55
Hot Channel & Hot Spot Factor Example

## Slide 56
Core Design Walkthrough

## Slide 57
Reactor Design
The final reactor design necessarily represents a series of compromises between nuclear and thermal-hydraulic factors which all made in the interest of safety and economy.
In designing a reactor, there is overlap between those problem that are specifically nuclear
  The neutron flux
  Power distributions
  Transient behavior
Thermal Hydraulics
  Those factors involving the removal of heat from the system

## Slide 58
Reactor Design
Once core basic lattice has been determined from nuclear, hydraulic, and heat transfer, the overall size of core becomes a sole function of thermal considerations
Parameters
  Fuel temperature distribution (most important)
  Specific power
  Power density
  Heat flux

## Slide 59
Reactor Design
Consider the design of a specified type of power reactor having a given thermal power output.
The first problem is the selection of the core materials
  Chosen on previous experience, availability and cost
  The amount and enrichment of the fuel including estimates of core lifetime and radiation damage to the fuel elements.
Second, a fuel lattice arrangement is then computed for the proposed fuel.
  The operating parameters of the reactor-the neutron flux,
  The power and temperature distributions,
  The coolant density and/or void distribution
  The temperature and heat flux along the hot channel

## Slide 60
Reactor Design
Such computations are inherently iterative, at least for some types of reactors.
With the PWR and BWR, it is necessary to know the water density as a function of position to compute the neutron flux and the power distribution.
However, the power distribution must be known before the water density.
We must assume some density distribution to start with, say, unity throughout the core.
The flux and power distributions are computed with this water density and a new density distribution is determined from the computed heat flux.

## Slide 61
Reactor Design
The neutron flux and power distributions are now computed using this new density distribution, and this in turn leads to a third density distribution.
The calculations are obtained until the density distribution provides a power distribution that gives the same density distribution.

## Slide 62
Reactor Design
During early stage in the design of the core, the neutron flux is usually obtained from a multigroup diffusion calculation using only a few groups.
To reduce computation costs, multigroup calculations with many groups are normally performed in the final stages of the design.
If the reactor is water cooled, the DNB ratio is next computed as a function of distance along the hottest channel.
The minimum DNBR must equal to some preset limiting value.

## Slide 63
Reactor Design
If the computed DNBR is not equal to this value then the parameters of the lattice or the coolant flow are changed, the previous calculations of the core are repeated and a new DNBR is obtained.
These computations are repeated until minimum value of DNBR is found.
Also determines the maximum heat flux, does not necessarily occur at the point where the DNBR is smallest.

## Slide 64
Reactor Design
If the reactor is not water cooled, is determined solely by the limiting value of the fuel temperature,
The overall hot channel factor, F, is obtained using the methods discussed earlier. The average heat flux throughout the core can then be computed from
This provides the reactor with the desired margin of safety.
(8)

## Slide 65
Reactor Design
Once is known, the total heat transfer area can be found from
Finally, from the heat transfer and the dimensions of the fuel rods, it is possible to compute the total number of rods required in the reactor.
(8)
(9)
(10)
& : are the fuel material diameter and density
: total length
: total mass

## Slide 66
Reactor Design
This number will undoubtedly be different from the one used at the start of the design.
Many of the foregoing calculations must be repeated until a completely self-consistent reactor is obtained.
At this point, detailed multigroup and two-dimensional neutron diffusion calculations can be undertaken, along with various transient analyses and lifetime-burnup computations, to refine the design.

## Slide 67
Reactor Design Exercise
A PWR has a core consists of fuel rods 10 ft long and 0.6 in. in diameter. The reactor operates at a thermal power of 3,000 MW; it has a maximum calculated heat flux of 539,000 Btu/hr- and an overall hot channel factor of 2.80. Calculate the total heat transfer area and the number of fuel rods in the core.
The average heat flux is given by:

## Slide 68
With the reactor power of 3,000 MWt = the heat transfer area is
Reactor Design Exercise
The surface area of each fuel rod is 10
The total number of rods is then

## Slide 69
Plant and Core Thermal Design Procedure

## Slide 70
Core Thermal Design
Reactor cores generate hundreds or thousands of megawatts (thermal)
The temperature anywhere in the core must not exceed material property limitations.
This is done by adjusting the fuel quality and surface area so that the heat fluxes do not result in temperatures exceeding these limitations.
The size of power reactor is therefore very large and prevented from becoming supercritical by proper design on the reactor-core system.
With such large sizes, the neutron leakage is small and nuclear considerations are no longer sensitive to changes in core size.

## Slide 71
Core Thermal Design
The detailed design of a core, however is a compromise between
  nuclear,
  material,
  structural,
  hydraulic,
  heat-transfer,
  economic
considerations, usually involving on iterative procedure to arrive at an optimum.

## Slide 72
Core Thermal Design
The most important parameter in the thermal design (hydraulic and heat transfer) is the fuel temperature distribution.
The specific power (kW(t)/kg), power density (kW(t)/liter) and heat flux (Btu/hr ) for once a basic fuel lattice have chosen.
They must be limited so that, together with the designed heat removal system (h) they would not result in temperatures that exceed fuel element material limitations and therefore in fuel element failure.

## Slide 73
In thermally designing a core one begins with several basic requirements, obtained from the power plant and steam cycle as the following:
The net power output in MW(e) is determined by the electric utility ordering the plant, based on demand.
The type of reactor is selected by the electric utility based on competitive or sometimes on a desire to gain experience in a new field or type of power plant or reactor.
The system cycle is designed, including the number of feedwater heaters, reheat stages, etc,. and the main and auxiliary power components selected and the main steam conditions established.
Plant and Core Thermal Design
Procedure

## Slide 74
Based on previous parameters, the net thermal efficiency of the power plant is determined.
The reactor output in MW(t) is now computed.
A basic fuel lattice (cell or subassembly) is determined from nuclear, hydraulic and heat-transfer considerations.
  These include fuel type and enrichment, cladding, fuel elment diameter, moderator to fuel ratio, etc.
  Often the choice of fuel type and fuel element diameter are predicted on the existence of manufacturing facilities for a particular type and size.
Reactor and Core Thermal Design
Procedure

## Slide 75
For a liquid-cooled core (PWR, BWR, etc.), a critical (burnout) heat flux is obtained from appropriate data or correlation. This may be reduced by a safety margin
An overall hot-spot factor is determined.
The core average heat flux, may now be determined
(11)
Reactor and Core Thermal Design
Procedure

## Slide 76
From , the total heat transfer surface (cladding surface) are , is determined
From the known fuel element cladding diameter the total length, , and total mass, , of the fuel are determined
(11)
: is the total thermal energy output of the core, obtained in step 5
(9)
(10)
& : are the fuel material diameter and density
: total length
: total mass
Reactor and Core Thermal Design
Procedure

## Slide 77
The overall core shape is now determined, e.g., an upright cylinder of a certain height to diameter ratio, commensurate with pressure drops, reactor pressure vessel diameter, etc.
The maximum fuel cladding and centre line temperatures are now checked using the individual hot-spot factors to ascertain that they do not exceed material limitations
Further reading on max temperature:
https://www.nuclear-power.net/nuclear-engineering/heat-transfer/heat-generation/temperature-profile-nuclear-fuel/
https://allthingsnuclear.org/dlochbaum/nuclear-safety-temperature-calculations-wheres-jethro/
Reactor and Core Thermal Design
Procedure

## Slide 78
The number and type of the control rods, are designed into the system and checked against nuclear, control and excess reactivity requirements for the new and equilibrium cores, e.g., a certain excess reactivity should be built into the core to overcome fuel depletion effects and still maintain good control rod position in the core.
The reactor vessel, core support structure, thermal shields, biological shields, etc. are now designed
Reactor and Core Thermal Design
Procedure

## Slide 79: References
Todreas, Kazimi, Nuclear Systems, Thermal Hydraulic Fundamentals, CRC Press
Lamarsh, Introduction to Nuclear Engineering, Prentice-Hall
M M ElWakil, Nuclear Heat Transport, International Textbook Company
Buongiorno, Notes on Two Phase Flow, Boiling Heat Transfer, and Boiling Crises in PWRs and BWRs, MIT
Buongiorno, Boiling Crisis in LWRs, MIT
Reactor Thermal Engineering IIb, ITP @ JAEA, August 2010

## Slide 80: Classification of Plant States